## Exterior Plastics Repair Kit

### Content

BL-1009_055

| 1 | Plastic Cleaner | For cleaning and degreasing of plastic parts. |
| --- | --- | --- |
| 2 | Plastic Primer | For better adhesion between 2K plastic adhesive and plastic parts |
| 3 | Self-adhesive reinforcement tape | For reinforcing the rear side of the area, requiring repair. |
| 4 | Double Barrel Cartridge gun |  |
| 5 | Universal 2K plastic adhesive | For plastic repairs to be sanded and painted after 30 minutes or more. |
| 6 | Fast 2K plastic adhesive | For plastic repairs to be sanded and painted after 10 minutes. |
| 7 | Mixing tube | To ensure that components of 2K adhesive are mixed correctly. |
| 8 | Contour foil | To follow the contour lines of the exterior plastic surface. |

### Additional Items and Tools

- The following additional items and tools must be purchased separately:

- Power drill with inserts, to stop the crack from continuing.

- Cutter knife, to create a V-shape in the surface of the tear for increased adhesion.

- Power cutter, to be used instead of the cutter knife.

- Sandpaper with P180 grit, to roughen up/rub down the to be repaired areas.

- Sandpaper with P320 grit, for final finish of the surface before primering.

- Scissors

- Safety glasses, to be worn while drilling and grinding.

- Breathing mask, to be worn while grinding.

### Technical Data

|  | Plastic Adhesive Superfast | Plastic Adhesive Fast | Plastic Adhesive Universal | Transparent Plastic Adhesive |
| --- | --- | --- | --- | --- |
| Processing Period | 25 sec | 1.5 min | 3.5 min | 3 min |
| Can be sanded at 23° C after | 5 min | 10 min | 30 min | 30 min |
| Can be painted after | 5 min | 10 min | 30 min | 30 min |
| Shore hardness D | 79 | 79 | 79 | 40 |
| Colour | Black | Black | Black | Colourless |

NOTE:	This information should only be seen as containing recommendations based on our experience. A preliminary test must be carried out.

NOTE:	The adhesives are not suitable for PE (polyethylene), PP (polypropylene) and PTFE (polytetrafluorethylene). The transparent adhesive is suitable for PC (polycarbonate) and PMMA (polymethylmetacrylate/plexiglas).

NOTE:	Due to coatings and release agents used when manufacturing plastics, in some cases there may be adhesion problems. If necessary, check material compatibility in an inconspicuous place.

## Operation

- Spray the areas to be adhered with plastic cleaning agent and allow the agent to act for 2 minutes. Then wipe with a clean, dry, lint-free cloth.

BL-1009_020

BL-1009_021

- To avoid any parts from tearing, drill a hole at the end of the area to be repaired.

BL-1009_022

- Cut or mill out the front side of the tear in a V shape

BL-1009_023

- Sand down the front and rear area to be repaired using P180 sandpaper. Avoid heating up the area being sanded.

BL-1009_024

- Apply a thin layer of plastic primer to both sides and allow to air for 2 minutes (at 23° C).

BL-1009_025

- Cut the self-adhesive reinforcement tape to the required size for the repair.

BL-1009_026

### Applying Adhesive

- Depending on your own preferences, proceed with the repair procedure applying adhesive either from the front or back to the area to be repaired.

#### Applying Adhesive to the Front Side

- Stick the adhesive tape directly to the back of the damaged area.

BL-1009_027

- Depending on the sort of repair choose either Universal or Fast adhesive. To achieve a homogenous 1:1 mixture squeeze out 1…2 cm of the adhesive, then proceed with the gluing process.

BL-1009_028

- Apply the adhesive from the front through the tear. Make sure that the tip of the mixing tube always remains in the adhesive so that air bubbles cannot be formed.

BL-1009_029

- Smooth excess adhesive using the contour foil and a spatula.

BL-1009_030

### Applying Adhesive to the Back

- Depending on the sort of repair choose either Universal or Fast adhesive. To achieve a homogenous 1:1 mixture squeeze out 1…2 cm of the adhesive, then proceed with the gluing process.

BL-1009_028

- Apply the adhesive directly to the reinforcement tape. Make sure that the tip of the mixing tube always remains in the adhesive so that air bubbles are not formed.

BL-1009_031

- Press a matching piece of the contour foil against the front side of the crack.

BL-1009_032

- Carefully press the reinforcement tape with the adhesive onto the rear side of the repair area until the adhesive squeezes through the tear and onto the front of the object, and against the contour foil.

BL-1009_033

BL-1009_034

- Smooth excess adhesive using the contour foil and a spatula.

BL-1009_035

### For Both Repair Procedures

- After the adhesive has hardened, remove the contour foil and sand the surface using P180 sandpaper. Avoid heating up the area being sanded.

BL-1009_036

- Now use P320 sandpaper to smooth the area, before applying primer and final paint coat finish.

BL-1009_037

Notes: